Dibutyl phthalate

GB/11405-89

Chemical name：Dibutyl phthalate

Abbreviation：DBP

Cas:84-74-2

The major physical and chemical property：

Molecular formula:C16H22O4

Molecular Weight：278.4

Specific gravity：(D20,20℃)1.0484

Solidification Point：-35℃

Boiling Point：327℃

This product is a colorless-transparentoily liquid，flammable，fragrant of smell.It can dissolve in　Common organic solvents and hydrocarbon，not dissolve in water．

The Standard Of Product Quality (GB/11405-89)

Terms        index                           High-class         First-class       Qualified

Color number (Pa-Co)           ≤       20                    25                    60

Content of ester(%)               ≥       99.5                  99.0                99.0

Density(P20,g/cm3)                 1.044-1.048      1.044-1.048       1.044-1.048

Acidity(Phthalic acid)%                     0.010                 0.015            0.030

Loss of weight in heat-ing(%)   ≤      0.3                     0.5                 0.7

Flash Point(℃)                ≥                160                   160              160

Heat Stability (Pa-Co)         ≤             100                   --                --

Remark：The content of ester is guarantee indes,it can be selective examined by production unit．

uses：

This product is a high solvability plastisizer，it can dissolve many kinds of resins.It is major used as the plastisizer of PVC，can provide the PVC product  with good flexibility．It is also a good plastisizer of the nitrocellulose．It possesses good soft property when used in the production of the nitrocellulose dope．It also used as the plastisizer of polyvinyl acetate，alkyd resin，ethyl cellulose and polychloroprene,and can be used in the production of paint，synthetic leather，printing ink，celluloid，dye，pesticide，solvent，viscous agent，perfume，safety glass，etc．

Packing：

200kg packed in irom drum．

Caution：

This product is flammable，must be far away from fire source，stored in dry and ventilatory place，keep the container closed to prevent the water soaking