Diisobutyl phthalate

GB/11405-89

Chemical name：Diisobutyl phthalate

Abbreviation：DIBP

Cas:

The major physical and chemical property：

Molecular formula:C16H22O4

Molecular Weight：278.4

Specific gravity ：(D20,20℃)1.0484

Solidification Point：-50℃

Boiling Point：327℃

This product is a colorless-transparentoily liquid，combustible，fragrant of smell.It can dissolve in the common organic solventes and hydrocarbon，not dissolve in water．

The Standard Of Product Quality (GB/11405-89)

Terms       Index                        High-cla           First-class           Qualified

Color number (Pa-Co)             ≤          20                    50                      70

Content of ester(%)              ≥          99.0                  99.0                    99.0

Density(P20,g/cm3)                      1.036-1.043       1.036-1.043            1.036-1.043

Acidity(Phthalic acid)%                  0.010                0.015                   0.030

Loss of weight in heat-ing(%)    ≤           0.4                   0.5                      0.7

Flash Point(℃)                  ≥          155                  150                      150

Heat Stability (Pa-Co)           ≤          100                  200                      --

Uses：

This Prodcti is similar to DBP，excepting the higher volatility and higher loss of water extraction，so it can be used as the substiute of DBP，but it is not suitable for the production of the agricultural plastic film．It is major used as the plastisizer of PVC，and can provide the PVC products with better flexibility；It is a excellent plastisizer of the nitrocellulose，used in the production of the nitrocellusose dope，it possesses good soft property；It also can be used as the plastisizer of the polyvinyl acetate，alkyd resin，ethyl cellulose and polychloroprene；It also can be used in the production of the pains，synthetic leather，printing ink，celluloid，dye，pesticide and so on．