DI-2-ETHYLHEXYL ADIPATE

Dioctyl adipate, for short DOA.

CAS:103-23-1

Appearance transparent liquid, no suspended substance

Item Standard

premium product    first-grade product    salable product   typical value

content of ester, %      99.0                   99.0                  99.0            99.0

density(20),g/cm3                                                 0.925-0.927

acidity,mgKOH/g          0.1                    0.15                   0.2             0.1

flashing point,                                          192

moisture content,%                                    0.1

chroma,(platinum-cobalt)    30                  50                    120               30

refractive index(20)                                     1.447-1.449

viscosity(20),mPa.s                                        12-15

USES:

DOA is a typical freeze-resisting plasticizer. With high plasticizing efficiency and low color degradation when heated,

it is used in many resins like PVC, chloroethylene polymer, polystyrene and synthetic rubber, making the products have fine flexibility under low temperature, good light permanency and feeling. Together with primary plasticizers like DOP or DBP, it is usually used in freeze-resisting agricultural film, packaging film of refrigerated food, wires and cables, artificial leather, board, outdoor water pipes. When used in plastisol, the paste has low viscosity at the beginning and the viscosity is stable.

This product is allowed in the manufacture of food packaging materials in USA, France, Italy,Japan and Holland,etc.PACKING:                      180kg/drum