Dioctyl terephthalate (DOTP)

CAS:

ICSC:

Appearance     transparent oily liquid, no suspended substance

As a primary plasticizer, DOTP has fine electrical performance, freeze and heat resistance and high plasticizing efficiency.

Quality Standards

Item                                                 Standard

premium product     first-grade product       salable product     typical value

content of ester，%   99.0              99.0                    99.0                 99.50

density(20),g/cm3                                   0.981-0.986

acidity(by benzenedicarbon acid)  0.015              0.020                 0.015

flashing point,      210                205                     210

chroma,(platinum-cobalt)    50           100                    200                   50

loss on dry，%      0.1                 0.2                     0.25                  0.1

volume resistivity,                ×10 10.m 90 ------------- 90

It is fit to be plasticizer of PVC resin like PVC cable materials needing high insulation. This product can be blended with DOP in any proportion. When used in plastisol, it can reduce the viscosity and increase the storage life.

DI-2-ETHYLHEXYL ADIPATE