Sodium Fluoride

Formulae: NaF

Molecular Weight: 42

UN. NO.: 83015

H.S. CODE:2826.1100

Properties: White powder, soluble in water, slightly soluble in alcohol, poisonous. Uses: Be used as manufacture of enamel, vermin destroyer, rat poison; as insecticide, preservatives for wood and food, antiseptic in alcohol distillation.

Specification:

NaF content ≥ 98%

Moisture ≤0.5%

SO4 ≤0.1%

Water insolubles ≤0.7%

PH ≤0.1%

Sodium Carbonates ≤0.5%

SiO2 ≤0.5%

Packing: In bags of 25kg net each, with plastic lining.