Sodium Fluorosilicate ( Sodium Silicofluoride)

Formulae: Na2SiF6

Formulae:　Na2SiF6

Molecular Weight:　220.26

UN. NO.:　2674

HAZARD CLASS:6.1

H.S. CODE:2826.2000

Physical chemistry properties: Colorless, odorless, poisonous and hygroscopic hexa-square crystal. Relative density is 2.679. either dissolvable substances, but undissolved in alcohol. Solubility is acid is larger than in water. Decomposed as fluoride and silicon oxide in alkali solution. Decomposed as Sodium fluoride and silicon fluoride over 300℃.

Usage: It can be used as white-adding reagent of porcelain enamel and glass, melt-supporting reagent, antiseptic of wood, insecticide in agriculture, moisture absorption reagent of acid tolerance cement, solidification matter of natural latex products, supplement of electrode posit trilateral of zinc-ferric nickel, filling substance of plastic. Also used in artificial

Spec

Name of chemicals Content

Appearance White crystal

Na2SiF6(based on dried basis) ∶99%

Dissociation acid (as HCI)  ML :0.1%

Heavy metal(as Pb)  ML0.02%

Fe ML0.02%

Water undissolvable substance ÷0.4%

Lost weight of 105ìC dried ML0.30%

Passing through 250/um screen ∶90%

Package and transportation: Packed in two layers polyethylene knitting

Bag. Net weight 25kg Please pay attention to package bag for protecting

The bag damage and dampness in transportation