TRIOCTYL TRIMELLITATE（TOTM)

ABBRE:TOTM

Cas:

ICSC:

Molecular Farmula: C33H54O6

Molecular Weight:547

Relative Density: 0.987-0.997(20℃)

oil transparent liquid with a slight smell

Quality Specifications:

Color (APHA)           120Max

Acidity%               0.03Max

Ester content%         99.0Min

Flash pointoC          240Min

Loss on heating%       0.15Max

Density(p20oC)g/cm3   0.988-0.986

ResistanceΩ.cm        1×1012Min

Function and Use:

Trioctyl Trimellitate(TOTM),is a heat-resistant and durable plasticizer and it is suitable to be used in various plastic meterials such as polyvinyl chloride,chloroethylene copolymer,nitrocellulose,ethyl cellulose,polymethyl methylacrylate and so forth.

The plasticizing rate of product can be similar to phthalate type plasticity agent and the durability of it can be as good as polymeric plastifiers.Many properties such as low volitility,excellent extractability-proof,best resistance to change ability as well as best resistance to cold and clectrical property belong to this product that can be used in making the products which require heat-resestance and durability such as heat-resistant cable materials,sheet meterials and sealing washers et

3 Package:

In new galvanized iron drum of 180kGS net each.